Standard Custom Wafers

|  |  | 1” | 2” | 3” | 4” | 6” |
| --- | --- | --- | --- | --- | --- | --- |
| Crystal |  | CZ | CZ | CZ/FZ | CZ/FZ | CZ/FZ |
| Orientation CZ |  | 100,111,110 211,311,411 | 100,111,110 211,311,411 | 100,111,110 211,311,411 | 100,111,110 211,311,411 | 100,111 |
| Orientation FZ |  | Contact Sales | Contact Sales | 100,111,110 | 100,111,110 | 100,111 |
| Orientation Tolerance | Degree | 0.1° | 0.1° | 0.1° | 0.1° | 0.1° |
| Off Orientation | Degree | Any | Any | Any | Any | 0-10° |
| Resistivity CZ As | Ohm cm | 0.002-20 | 0.002-20 | 0.002-20 | 0.002-20 | Contact Sales |
| Resistivity CZ Ph | Ohm cm | 0.01-25 | 0.01-25 | 0.01-25 | 0.01-25 | 1-50 |
| Resistivity CZ Sb | Ohm cm | 0.006-0.02 | 0.006-0.02 | 0.006-0.02 | 0.006-0.02 | Contact Sales |
| Resistivity CZ Boron | Ohm cm | 0.001-50 | 0.001-50 | 0.001-50 | 0.001-50 | 0.5-50 |
| Resistivity CZ Undoped | Ohm cm | 20-500 | 20-500 | 20-500 | 20-500 | 20-500 |
| Resistivity FZ | Ohm cm | <5000 | <5000 | <5000 | <5000 | <5000 |
| Bow | Micron | <10.0 | <10.0 | <10.0 | <10.0 | <20.0 |
| Min. TTV | Micron | <1 | <1 | <1 | <1 | <1 |
| Thickness | Micron | 200-2500 | 200-2500 | 200-2500 | 200-2500 | 200-1000 |
| Thickness Tolerance | Micron | +- 15 | +- 15 | +- 15 | +- 15 | +- 15 |
| Minimum Surface Roughness | Angstrom | 5 | 5 | 5 | 5 | 5 |
| Surface Type | SSP,DSP Lapped | SSP,DSP Lapped | SSP,DSP Lapped | SSP,DSP Lapped | SSP,DSP Lapped | SSP,DSP Lapped |

Standard Ultra-Thin ® Wafers

|  |  | 1” | 2” | 3” | 4” | 6” |
| --- | --- | --- | --- | --- | --- | --- |
| Crystal |  | CZ | CZ | CZ/FZ | CZ/FZ | CZ/FZ |
| Thickness <100> | Micron | 10-190 | 8-190 | 8-190 | 8-190 | 50-190 |
| Thickness <110> | Micron | 25-190 | 25-190 | 25-190 | 25-190 | Contact Sales |
| Thickness <111> | Micron | 75-190 | 75-190 | 75-190 | 75-190 | Contact Sales |
| Minimum Surface Roughness | Angstrom | 5-50 | 50 | 50 | 50 | 50 |
| Thickness Tolerance | Micron | <15% | <15% | <15% | <15% | <15% |
| TTV | Micron | <2µm | <2µm | <2µm | <2µm | <2µm |

Full Custom Products

Any 1”-6” wafer or crystal can be made to virtually any specification as a custom order.  Also Bonded –(SOI) Wafers are available.

Bondedwafers.com