# Basic Mechanical and Thermal Properties of Silicon

Virginia Semiconductor, Inc.

1501 Powhatan Street, Fredericksburg, VA 22401

(540) 373-2900, FAX (540) 371-0371

www.vriginiasemi.com, tech@virginiasemi.com

### A Introduction

This paper outlines some of the basic mechanical and thermal properties of silicon.

B Crystalline Structure and Elastic Properties

Three values for the lattice parameter of pure Silicon at 22.500 °C are given below.  The values were determined in independent studies through  X-ray and optical interferometry (XROI).

a= 543102.032 +/- 0.033 fm [2]

a= 543102.044 +/- 0.017 fm [3]

a= 543101.99 +/- 0.09 fm     [4]

The value of the linear thermal expansion coefficient (α(T)) is given by the following expression:

α(T) = (3.725{1- exp[-5.88 x 10-3 (T – 124)]} + 0.5548 x 10-3T) x 10-6 K-1	[1]

where T is the absolute temperature expressed in Kelvin and valid for values of T between 120 K and 1500 K (SEVERAL RESEARCHERS HAVE QUESTIONED THE ACCURACY OF THIS EQUATION).  At 25.0 °C the recommended value is

α298.2 = (2.59 +/- 0.05) x 10-6 K-1

The lattice parameter at T K is given by

a(T) = a0 					[1]

where a0 is the lattice parameter at 295.7 K.

The second order lattice constants are related by [5]

σii = C11 εii  + C12 (εjj + εkk)

σii = 2C44 εij                (i ≠ j)

where σ represents stresses and ε represents elastic strains. The three constants at room temperature and atmospheric pressure are given below [6]

C11 = 1.6564 x 1011 Pa

C12 = .6394 x 1011 Pa

C44 = .7951 x 1011 Pa

Between 150 K and 1000 K the decrease of the Cij with increasing temperature is fairly linear and follows these rates:

= -9.4 x 10-5 K-1		[7]

= -9.3 x 10-5 K-1		[8]

= -9.8 x 10-5 K-1		[7]

= -8.3 x 10-5 K-1		7]

= -1.0 x 10-4 K-1		[8]

= -7.3 x 10-5 K-1		[8]

For further information on third order elastic constants and the effects of doping see [6].

### C Thermal Properties

Table 1 Thermal Expansion Coefficient [1]

| T (K) | α (10-6 K-1) | T (K) | α (10-6 K-1) | T (K) | α (10-6 K-1) |
| --- | --- | --- | --- | --- | --- |
| 5 | 0.6 x 10-4 | 180 | 1.061 | 700 | 4.016 |
| 10 | 0.48 x 10-3 | 200 | 1.406 | 800 | 4.151 |
| 20 | -0.29 x 10-2 | 220 | 1.715 | 900 | 4.185 |
| 40 | -0.164 | 240 | 1.986 | 1000 | 4.258 |
| 60 | -0.400 | 260 | 2.223 | 1100 | 4.323 |
| 80 | -0.472 | 280 | 2.432 | 1200 | 4.384 |
| 100 | -0.330 | 300 | 2.616 | 1300 | 4.442 |
| 120 | -0.057 | 400 | 3.253 | 1400 | 4.500 |
| 140 | 0.306 | 500 | 3.614 | 1500 | 4.556 |
| 160 | 0.689 | 600 | 3.842 | 1600 | 4.612 |

Table 2 Melting Temperatures [1]

| Temperature (°C) | 1408 | 1410 | 1412 | 1414 | 1416 |
| --- | --- | --- | --- | --- | --- |
| Number or Reports | 1 | 1 | 7 | 8 | 3 |

Table 2 summarizes the reported melting points since 1948 of silicon.  The melting point is extremely difficult to determine due to the calibration of the machinery and also the fact that molten silicon is highly reactive and most impurities serve to depress the melting point.  The mean of the data given above is 1413.2 °C with a standard error of 0.31 degrees.  Since the error in these measurements is negative, the best value to use would be one slightly higher than the mean, such as 1414.0 °C.  [1]

Table 3 Thermal Conductivity Values (Above 200 K) [9]

| T (K) | K (W cm-1 K-1) | T (K) | K (W cm-1 K-1) |
| --- | --- | --- | --- |
| 200 | 2.66 | 1000 | 0.31 |
| 300 | 1.56 | 1100 | 0.28 |
| 400 | 1.05 | 1200 | 0.26 |
| 500 | 0.80 | 1300 | 0.25 |
| 600 | 0.64 | 1400 | 0.24 |
| 700 | 0.52 | 1500 | 0.23 |
| 800 | 0.43 | 1600 | 0.22 |
| 900 | 0.36 | 1681 | 0.22 |

Table 4 Thermal Conductivity Values (Below 200 K) [10]

| T (K) | K (W cm-1 K-1) | T (K) | K (W cm-1 K-1) |
| --- | --- | --- | --- |
| 150 | 4.10 | 20 | 47.7 |
| 100 | 9.13 | 10 | 24.0 |
| 50 | 28.0 | 8 | 16.4 |
| 40 | 36.6 | 6 | 8.99 |
| 30 | 44.2 | 4 | 3.11 |
|  |  | 2 | 0.44 |

Table 4 Maximum Thermal Conductivity Versus Concentration of Boron Impurities [1][10]

|  | Thermal Conductivity |  |
| --- | --- | --- |
| Boron Concentration (cm-3) | Maximum (W cm-1 K-1) | Temperature (K) | Sample cross-section (mm2) |
| 1.0 x 1013 | 48 | 22 | 6.03 x 6.07 |
| 4.2 x 1014 | 43 | 25 | 6.17 x 6.32 |
| 4.2 x 1014 | 38 | 26 | 3.45 x 3.50 |
| 1.0 x 1015 | 43 | 25 | 6.19 x 6.32 |
| 4.0 x 1015 | 33 | 27 | 5.86 x 5.86 |
| 4.0 x 1016 | 18 | 37 | 6.24 x 6.27 |

Table 5 Thermal Diffusivity (Above 300 K) [11]

| T (K) | D(cm2 s-1) | T(K) | D(cm2 s-1) |
| --- | --- | --- | --- |
| 300 | 0.86 | 800 | 0.19 |
| 400 | 0.52 | 900 | 0.16 |
| 500 | 0.37 | 1000 | 0.14 |
| 600 | 0.29 | 1200 | 0.12 |
| 700 | 0.24 | 1400 | 0.12 |

Table 6 Thermal Diffusivity (Below 300 K) [12]

| T (K) | D(cm2 s-1) | T(K) | D(cm2 s-1) |
| --- | --- | --- | --- |
| 50 | 63.5 | 100 | 11.3 |
| 60 | 37.6 | 150 | 4.24 |
| 70 | 24.8 | 200 | 2.23 |
| 80 | 17.1 | 250 | 1.23 |
| 90 | 14.4 |  |  |

For information on the heat for fusion for silicon, see [13][14]

For information on the surface tension of liquid silicon, see [15]

### D Conclusion

This paper contained information on basic mechanical and thermal properties of silicon.

### E References

[1]	R. Hull [ Properties of Crystalline Silicon (INSPEC, London, 1999)]

[2]	D. Windisch, P. Becker [ Phys. Status Solidi A (Germany) vol.118 (1990) p.379]

[3]	G. Basile, A. Bergamin, G. Cavagnero, G. Mana, E. Vittone, G. Zosi [Phys. Rev. Lett. (USA) vol.72 (1994) p. 3133]

[4]	H. Fujimoto, K. Nakayama, M. Tanaka, G. Misawa [Jpn. J. Appl. Phys. (Japan) vol.34 (1995) p.5065]

[5]	C. Kittel [Introduction to Solid State Physics 4th Edn (Wiley, 1971) ch.4]

[6]	J.J. Hall [ Phys. Rev. (USA) vol.161 (1967) p.756]

[7]	[ Landolt-Bornstien Numverical Data and Functional Relationships in Science and Technology, New Series, Ed. K.H. Hellwidge (Springer Verlag, Germany, 1979) vol. 17 and 22]

[8]	Yu.A. Burenkov, S.P. Nikanorov [Sov. Phys.-Solid State (USA) vol.16 (1974) p.963]

[9]	C.J. Glassbrenner, G.A. Slack [ Phys. Rev. (USA) vol.134 (1964) p.A1058]

[10]	M.G. Holland, L.G. Nueringer [ Proc. Int. Conf. Physics if Semiconductors, Exeter, England, 1962 (Inst. Phys., Bristol, 1962) p. 474]

[11]	B. Abeles, D.S. Beers, G.D. Cody, J.P. Dismukes [Phys. Rev. (USA) vol.125 (1962) p.44]

[12]	P. Turkes [ Phys. Status Solidi A (Germany) vol.75 no.2 (1983) p.519-23]

[13]	R.R. Hultgren et al [ Selected Values of Thermodynamic Properties of Metals and Alloys (Wiley, New York, 1968)]

[14]	 R.R. Hultgren et al [ Selected Values of Chemical Thermodynamic Properties of Elements (Wiley, New York, 1973)]

[15]	S.C. Hardy [ J. Cryst. Growth (Netherlands) vol.69 no.2/3 (1984) p.456-60]