# VSI Specification for SOI Wafers

## Bonded Wafers Specifications

Wafer Properties		                             Target Specifications

| Thermal SiO2 Layer Thickness | 0.5µm-4.0µm |
| --- | --- |
| Handle Wafer Thickness | 250µm – 1000µm |
| Device Wafer Thickness | 10µm – 525µm |
| Device Wafer Tolerance | 0.5µm – 25µm |
| Device and Handle Wafer Resistivities | 0.01-100 Ohm-cm |
| Crystal Orientation & Dopant | ANY |
| Wafer Diameter | 100mm & 150mm |