The General Properties of Si, Ge, SiGe, SiO2 and Si3N4

## June 2002

## Virginia Semiconductor

## 1501 Powhatan Street, Fredericksburg, VA 22401-4647 USA

Phone: (540) 373-2900, FAX (540) 371-0371

www.virginiasemi.com, tech@virginiasemi.com

A. Introduction

### This paper summarizes basic physical properties of   Si, Ge, SiGe, SiO2 and Si3N4. It also lists several physical constants and conversion factors.  The information is presented in table format with explanations of any approximations or equations used.

#### B. The Basic Properties of Si, Ge, and SiGe

The following table summarizes many of the basic physical properties of Silicon, Germanium, and Silicon Germanium at different concentrations.  The concentrations are given in the form of Si1-xGex where x represents the percent composition of Germanium.

| Properties | Ge | Si.25Ge.75 | Si.5Ge.5 | Si.75Ge.25 | Si |
| --- | --- | --- | --- | --- | --- |
| Atoms/cm3 | 4.42 x 1022 Ge | *4.415 x 1022 | *4.61 x 1022 | *4.805 x 1022 | 5.0 x 1022 Si |
| Atomic weight | 72.60 Ge | *61.4725 | *50.345 | *39.2175 | 28.09 Si |
| Breakdown field (V/cm) | ~105 Ge | *1.5 x 105 | *2 x 105 | *2.5 x 105 | ~3 x 105 Si |
| Crystal Structure | Diamond | Diamond | Diamond | Diamond | Diamond |
| Density (g/cm3) | 5.3267 Ge | *4.577 | *3.827 | *3.078 | 2.328 Si |
| Dielectric constant | 16.0 Ge | *14.975 | *13.95 | *12.925 | 11.9 Si |
| Effective density of States in conduction band, Nc (cm-3) | 1.04 x 1019 Ge |  |  |  | 2.8 x 1019 Si |
| Effective density of States in valence band, Nv (cm-3) | 6.0 x 1018 Ge |  |  |  | 1.04 x 1019 Si |
| Effective Mass, m*/ m0 Electrons Holes | m*l= 1.64 m*t= 0.082 m*l h= 0.044 m*h h= 0.28 Ge |  |  |  | m*l= 0.98 m*t= 0.19 m*l h= 0.16 m*h h= 0.49 Si |
| Electron affinity X(V) | 4.0 Ge | *4.0125 | *4.025 | *4.0375 | 4.05 Si |
| Minimum Indirect Energy Gap (eV) at 300K | 0.66 Ge | ***0.804 | ***0.945 | ***1.05 | 1.12 Si |
| Minimum Direct Energy Gap (eV) | .7 Ge | 1.6 | 2.5 | 3.1 | 3.4 Si |
| Intrinsic carrier concentration (cm-3) | 2.4 x 1013 Ge | *1.8 x 1013 | *1.2 x 1013 | *0.6 x 1013 | 1.45 x 1010 Si |
| Intrinsic Debye length (μm) | 0.68 Ge | *6.51 | *12.34 | *18.17 | 24 Si |
| Intrinsic resistivity (Ω-cm) | 47 Ge | *.575 x 105 | *1.15 x 105 | *1.725 x 105 | 2.3 x 105 Si |
| Lattice Constant (A) | ***5.6575 Ge | ***5.5960 | ***5.5373 | ***5.4825 | ***5.4310 Si |
| Linear coefficient of thermal expansion, ΔL/LΔT ((C-1) | 5.8 x 10-6 Ge | *5.0 x 10-6 | *4.2 x 10-6 | *3.4 x 10-6 | 2.6 x 10-6 Si |
| Melting point ((C) | 937 Ge | *1056.5 | *1176 | *1295.5 | 1415 Si |
| Minority carrier lifetime (s) | 10-3 Ge | *1.375 x 10-3 | *1.75 x 10-3 | *2.125 x 10-3 | 2.5 x 10-3 Si |
| Mobility (drift) (cm2/V-s) | 3900(electron) 1900(hole) Ge | *3300(electron) *1537.5(hole) | *7700(electron) *1175(hole) | *2100(electron) *812.5(hole) | 1500(electron) 450(hole) Si |
| Optical – phonon energy (eV) | 0.037 Ge |  |  |  | 0.063 Si |
| Phonon mean free path λ0(Å) | 105 Ge |  |  |  | 76 (electron) 55 (hole) Si |
| Specific heat (J/g-(C) | 0.31 Ge | *.4075 | *.505 | *.6025 | 0.7 Si |
| Thermal conductivity at 300 K (W/cm-(C) | 0.6 Ge | **.11 | **.083 | **.085 | 1.5 Si |
| Thermal diffusivity (cm2/s) | 0.36 Ge | *0.495 | *.63 | *.765 | 0.9 Si |
| Vapor pressure (Pa) | 1 at 1330(C 10-6 at 760(C Ge | 1 at *1410(C 10-6 at *795 | 1 at *1490(C 10-6 at *830(C | 1 at *1570(C 10-6 at *865(C | 1 at 1650(C 10-6 at 900(C Si |

*  value was derived through linear approximation  ; **  value was derived through subjective observation of graph/diagram  [1]; ***  value was derived through quadratic approximation

###### TABLE 1 lists physical properties of Si, Ge, and SiGe [2][3]

### The linear approximations were calculated using the following function where CSi represents the Silicon value,  CGe represents the Germanium value, and x represents the fractional composition of Germanium:

a(x)= CSi (1-x) + CGe (x).

All values in the above table for SiGe are %atm values.  The values for the thermal conductivity were taken from a graph[1][7].  The values for the minimum indirect energy gap were determined from both a graph[1][8] and also from the following quadratic expression where  x represents the fractional composition of Germanium:

#### Eg(x)= (1.155 – 0.43x + 0.0206x2 )eV	for	0 < x < 0.85	[1][5]

and

Eg(x)= (2.010 – 1.27x)eV        		for  	0.85 < x < 1	[1][5]

The values for the minimum direct energy gap were determined from references [1],[6].

The lattice constants were determined using the following quadratic expression where x represents the percent of Germanium in the composition:

a(x) = 0.002733x2 + 0.01992x + 0.5431 (nm)[9].

#### C. The Basic Properties of SiO2 and Si3N4

| Insulator: | SiO2 | Si3N4 |
| --- | --- | --- |
| Structure | Amorphous | Amorphous |
| Melting Point ((C) | ~1600 | - |
| Density (g/cm3) | 2.2 | 3.1 |
| Refractive index | 1.46 | 2.05 |
| Dielectric constant | 3.9 | 7.5 |
| Dielectric strength (V/cm) | 107 | 107 |
| Infrared absorption band (μm) | 9.3 | 11.5 – 12.0 |
| Energy gap | 9 | ~5.0 |
| Thermal Expansion coefficient ((C-1) | 5 x 10-7 | - |
| Thermal conductivity (W/cm-K) | 0.014 | - |
| dc resistivity (Ω-cm) at 25 (C at 500 (C | 1014 -1016 - | ~1014 ~2 x 1013 |
| Etch rate in Buffered HFa (Å/min) | 1000 | 5-10 |

a Buffered HF: 34.6% (wt.) NH4F, 6.8% (wt.) HF, 58.6% H20

TABLE 2 lists physical properties of SiO2 and Si3N4. [ 2]

#### D. Physical Constants

| Symbol | Name | Value |
| --- | --- | --- |
| q | magnitude of electronic charge | 1.602 x 10-19 C |
| M0 | electron mass in free space | 9.109 x 10-31 kg |
| Eo | permittivity of vacuum | 8.854 x 10-14 F/cm |
| k | Boltzmann’s constant | 1.381 x 10-23 J/K 8.617 x 10-5 eV/K |
| h | Planck’s constant | 6.625 x 10-34 J-s 4.135 x 10-15 eV-s |
| KT | thermal energy | 0.02586 eV (T = 27 (C) 0.02526 eV (T = 20 (C) 0.026 eV ( room temperature) |

TABLE 3 lists the symbols for several common physical constants

and gives their value. [4]

E. Conversion Factors

| 1 Å | = 10-8 cm = 10-10 m |
| --- | --- |
| 1 μm | = 10-4 cm = 10-6 m |
| 1 mil | = 10-3 in = 25.4 μm |
| 1 mil2 | = 645.2 μm2 = 6.45 x 10-6 cm2 |
| 1 eV | = 1.602 x 10-19 J |

###### TABLE 4 list several common conversion factors.[4]

F. Conclusion

### In this paper the basic properties of    Si, Ge, SiGe, SiO2 and Si3N4 were reviewed along with useful physical constants and conversion factors. Some data was taken directly from reference while other values were derived using linear and quadratic expressions.

### G. References

[1]	E. Kasper [ Properties of Strained and Relaxed Silicon Germanium (INSPEC, London, 1995)]

[2] 	S.M. Sze [ Physics of Semiconductor Devices (John Wiley and Sons, Inc, New York, 1981)]

[3] 	S. Wolf, R. Tauber [ Silicon Processing for the VLSI Era (Lattice Press, Sunset Beach, California, 1986)]

[4]	G. Neudeck [ The PN Junction Diode ( Addison-Wesley Publishing Co., Reading, Massachusetts, 1989)]

[5]	J. Weber, M.I. Alonso [ Phys. Rev. B (USA) vol. 40 (1989) p. 5683]

[6]	P. Etchegoin, J. Kircher, M. Cardona, C. Grein [ Phys. Rev. B (USA) vol. 45 (1992) p. 11721];

P. Etchegoin, J. Kircher, M. Cardona[ Phys. Rev. B (USA) vol. 47 (1993) p. 10292];

[7]	J.P. Dismukes, L. Ekstrom, E.F. Steigmeier, I. Kudman, D.S. Beers [ J. Appl. Phys. (USA) vol. 35 (1964) p. 2899]

[8]	R. Braustein, A.R. Moor, F. Herman [Phys. Rev. (USA) vol. 109 (1958) p.695]

[9]	J.P. Dismukes, L. Ekstrom, R.J. Paff [ J. Phys. Chem. (USA) vol.68 (1964) p.3021-7 ]